ISO 9001:2008 Certified Company

Manufacturer’s Specifications

SportBase™ Tiles

Product Description

SportBase is a heavy-duty, easy to install, modular sub-base flooring system that is designed for outdoor weatherability, is environmentally friendly, and promotes water drainage.  SportBase provides a stable, high performance base for installing Sport Court modular products anywhere.

Technical Information

Dimensions:				18” x 18” x 2” square puzzle piece design

Weight:				6.4 lbs.

Material:				100% Recycled material

Polyolefin thermoplastic	50-100%

Other thermoplastic		0-50%

Non-thermoplastic		0-50%

Color:					Black with colored specks

Connection System:			Corner locks snap in to connect 4 tiles

Edge locks snap in to connect perimeter tiles

Locks made in high-strength nylon

Performance Test Results*

Force Reduction:			37% (DIN 18032-02:2004)

Ball Rebound:				96% (DIN 18032-02:2004)

*System tested with PowerGame™ tiles over 8” compacted sand sub-base

Optional Accessories:			Corner lock removal tool

Warranty:				10 year limited